SECTION 04 22 00

SELF-ADHERING SHEET FLASHING

PART 1  GENERAL

1.01	SECTION INCLUDES

A.	Flexible sheet membrane, including:

1.	Flexible self-adhering flashing membrane.

2.	Other specified system accessories.

1.03	REFERENCE STANDARDS

A.	ASTM D903 - Standard Test Method for Peel or Stripping Strength of Adhesive Bonds

B.	ASTM C765 - Standard Test Method for Low-Temperature Flexibility of Preformed Tape Sealants.

C.	ASTM E96 - Standard Test Methods for Water Vapor Transmission of Materials

D.	ASTM D412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers--Tension.

E.	ASTM D1970/D1970M - Standard Specification for Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection.

F.	ASTM E154/E154M - Standard Test Methods for Water Vapor Retarders Used in Contact with Earth Under Concrete Slabs, on Walls, or as Ground Cover.

G.	ASTM E2178 - Standard Test Method for Air Permeance of Building Materials.

H.    ASTM D570 - Standard Test Method for Water Absorption of Plastics

1.04	ADMINISTRATIVE REQUIREMENTS

A.	Coordination:

1.	Coordinate the installation of flexible self-adhering membrane with adjacent flashings, waterproofing systems, and other weather barriers for compatibility and continuity of those systems.

2.	Coordinate installation of flexible self-adhering membrane at openings with Sections that specify window, door, and other opening installations.

B.	Preinstallation Meeting:  Conduct a preinstallation meeting one week prior to the start of the work of this Section; require attendance by all affected installers.

1.	Discuss installation procedures, requirements for items that penetrate the system, and other pertinent issues.

1.05	SUBMITTALS

A.	Product Data:  Provide data on material characteristics, performance criteria, and limitations.

B.	Shop Drawings:  Provide drawings of special joint conditions, including special conditions where incompatible materials are in close proximity to or in contact with specified metal sheet flashings.

C.	Manufacturer's Installation Instructions:  Indicate installation methods, and storage and handling criteria.

1.06	QUALITY ASSURANCE

A.	Installer Qualifications:  Company specializing in performing the work of this Section with minimum three years documented experience, and approved by manufacturer.

B.	System Compatibility:  Assume responsibility for confirming that flexible self-adhering membrane is compatible with substrate surfaces with which they will be in contact, including but not limited to wall and sheathing surfaces, opening materials, waterproofing systems, other flashings and weather barrier materials, and sealants.

1.	Assure that system components are compatible as specified prior to preparing and making specified submittals.

2.	Assume responsibility for removal of incompatible system components and installation of properly compatible components at no additional cost to Owner regardless of when incompatibility is discovered.

C.	Basis of Design:  Specifications are based on flexible self-adhering membrane product by specified basis of design manufacturer.  Flexible self-adhering membrane product manufactured by other acceptable manufacturers are permitted, subject to compliance with specified requirements; and provided that deviations in design and performance are minor, and do not detract substantially from the indicated design intent.

1.07	MOCK-UPS

A.	Mock-up:  Construct mock-up of representative installation condition(s) as directed by Architect, indicating installation conditions including complete flashing application.

1.	Locate where directed.

2.	Mock-up may remain as part of work.

PART 2  PRODUCTS

2.01	FLEXIBLE SHEET FLASHINGS

===========================================================================

<<<<  RETAIN ONLY SALIENT CHARACTERISTIC PARAGRAPHS THAT ARE RELEVANT TO APPLICATION.

===========================================================================

A.	Flexible Self-Adhering Membrane:  Self-adhering, composite polyethylene and proprietary high temperature adhesive sheet membrane composed of UV-resistant woven polyethylene top sheet, proprietary high temperature adhesive, and release sheet; inherently compatible with all known underlayment and air barrier sheets, membranes, and coatings; requiring no substrate surface primers prior to installation; 120 day maximum weather and UV exposure.

1.	Application Temperature of Substrates:  20 degrees F to 120 degrees F.

2.	Composite Sheet Membrane:

a.	Woven Polyethylene Top Sheet

b.	Composite Hot-Melt Adhesive

c.	Total Sheet Thickness:  40 mil, 0.040 inch.

3.	Tensile Strength:  Pass, minimum 6,182 psi; tested in accordance with ASTM D412.

4.	Pliability:  Pass; tested in accordance with ASTM C765.

5.	Puncture Resistance:  337 lbf, minimum; tested in accordance with ASTM E154/E154M.

6.	Fastener Sealability:  Pass; tested in accordance with ASTM D1970/D1970M.

7.	Peel Strength:  Minimum 10 lbf on application substrates; tested in accordance with ASTM D570.

8.	Basis of Design Product:

a.	York Manufacturing, Inc.; Flexo-Flash:  www.yorkflashings.com.

9.	Other Acceptable Products:

a.	3 GEN Masonry Products; GENFLASH: www.3genmp.com.

b.	MortarNet; MortarFlash: www.mortarnet.com.

c.     Hohmann & Barnard; Textroflash: www.h-b.com/products/textroflash-flashing.

d.     Wire-Bond; MAS-N-FLASH: www.wirebond.com.

e.	Substitutions:  Permitted in accordance with Substitution Procedures specified in Division 01.

B.	Accessory Components:  As recommended by manufacturer for indicated applications.

PART 3  EXECUTION

3.01	EXAMINATION

A.	Verify that surfaces and conditions are ready for work of this Section.

B.	Where existing conditions are responsibility of another installer, notify Architect of unsatisfactory conditions.

C.	Do not proceed with this work until unsatisfactory conditions have been corrected.

3.02	PREPARATION

A.	Remove projections, protruding fasteners, and loose or foreign matter that might interfere with proper installation and adhesion of sheet membrane.

3.03	INSTALLATION

A.	General:  Install self-adhering flexible sheet membrane materials in accordance with manufacturer's published installation instructions for each indicated application.

1.	Installation instructions are available at:  https://www.yorkflashings.com/products/flexo-flash

B.	Comply with manufacturer's protocols and special application instructions, particularly for cold-weather applications.

C.	Once sheets are in place, press firmly into substrate; ensure that laps are firmly adhered with no gaps or fish mouths.

3.04	FIELD QUALITY CONTROL

A.	Do not cover installed membrane until required inspections have been completed.

B.	Obtain approval of installation procedures from membrane manufacturer based on a mock-up installed in place, prior to proceeding with remainder of installation.

C.	Take digital photographs of each portion of installation prior to covering up installed flashings.

3.05	PROTECTION

A.	Protect installed membranes from damage and integrity of sheet metal layer until covered by subsequent construction.

END OF SECTION