# SECTION 07 6500

# SELF-ADHERING DETAIL FLASHING

PART 1 - GENERAL

1.01	SUMMARY

A.	Flexible self-adhering butyl detail flashing.

EDIT RELATED SECTIONS TO INCLUDE ONLY SECTIONS IN PROJECT MANUAL.

1.02	REFERENCES

A. 	ASTM - American Society for Testing and Materials

1. ASTM E96 – Test Methods for Water Vapor Transmission of Materials

2. ASTM D570 – Test Method for Water Absorption of Plastics

3. ASTM E2112 – Standard Practice for Installation of Exterior Windows, Doors, and Skylights

4. ASTM D1970 – Standard Specifications for Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection

5. D412 – Test Methods for Vulcanized Rubber & Thermoplastic Rubbers and Thermoplastic Elastomers – Tension

6.  ASTM D3652 – Standard Test Method for Thickness of Pressure Sensitive Tapes

B.  AAMA – American Architectural Manufacturers Association

1.  AAMA 711-13 Voluntary specification for self-adhering flashing used for installation of exterior wall fenestration products.

1.03	SUBMITTALS

A.	Product data:  Indicate material type, composition, thickness, and installation procedures.

B.	Samples:  3" by 5" flashing material.

C.	Test reports indicating compliance with the performance requirements of this section.

1.04	QUALITY ASSURANCE

A.	Qualifications:

1.	Manufacturer:  Provide flashing materials by single manufacturer with not less than twenty-five years of experience in manufacturing flexible flashing products.

2. 	Warranty period is five years from the date of completion of the installation. Flashing will be free of defects at the time of delivery and are manufactured to meet manufacturer’s published physical material specifications and properties.

3.  Delivery and storage must comply with the manufacturer’s recommendations for handling and storage of the products.

1.05	QUALITY ASSURANCE

A.	Qualifications:

1.	Manufacturer:  Provide flashing materials by single manufacturer with not less than twenty five years of experience in manufacturing flexible flashing products.

SPECIFIER’S NOTE:  All manufacturers of air barrier, insulation and flashing products should provide you MUTUAL letters of compatibility for these products in combination with each other.  (York has these on file for you.)

1.06	WARRANTY

A.	Special warranty:

1.	Manufacturer:  Warrant flexible flashing material for 5 years.

2.	Begin warranty at Date of Substantial Completion.

### PART 2 — PRODUCTS

2.01 	MATERIALS

A. 	Flashing Description: 10mils of a white colored non-asphaltic, butyl-modified, adhesive integrally bonded to 4mils of engineered polypropylene film, which makes this a 14 mil thick membrane. Membrane has a silicone-coated release linear and this should remain on the flashing until it is installed.

B. 	Performance Requirements:

- Meets or exceeds the requirements set forth in AAMA 711-13 voluntary specification for self-adhered flashing Level 3 requirement for elevated temperature exposure.

- Meets or exceeds the requirements set forth in ASTM E2112 for Flashing Exterior Windows and Doors

- Water Penetration around Nails: ASTM D1970 Section 7.9, modified per section 5.2.1 of AAMA 711 voluntary specification – Pass 1.2 in head of water

- Tensile Strength: ASTM D412, Die C Modified – Min. 985 kPa (143 psi)

- Thickness:  ASTM 3652 – Min 14 mils

- Color: Visual inspection – White film

C.	Product: York Max-Seal butyl tape

D.	Flashing Accessories:

1. 	Primer: if the substrate surface is not appropriately free of contaminants or that field testing produced lower than desirable adhesion, then we would recommend a primer be used.  When required by dirty or dusty site conditions or by surfaces having irregular or rough texture, apply primer by air spray, brush or roller or apply at the rate recommended by manufacturer, prior to flashing installation. Allow the primer to dry completely before flashing application.

### PART 3 — EXECUTION

3.01 	EXAMINATION

A. 	Examine conditions, with installer present, for compliance with requirements for installation, tolerances and other specific conditions affecting performance of flashing. Remove all deleterious materials from surfaces to be flashed.

3.02 	INSTALLATION

- General: Install flashing to dry surfaces at air and surface temperatures of -4ºC (25ºF) and above in accordance with manufacturer’s recommendations at locations indicated on Construction Documents.  Primer is not required for most substrates including plywood provided they are clean and dry.  On concrete, masonry, and exterior gypsum apply primer prior to flashing if field testing showed lower than desired adhesion.

B. 	Flexible Wall Flashing:

1. 	Precut pieces of flashing to easily handled lengths for each location.

2. 	Remove silicone-coated release linear and position flashing carefully before placing it against the surface.

3. 	When properly positioned, place against surface by pressing firmly into place by hand roller. Fully adhere flashing to substrate to prevent water from migrating under flashing.

4. 	Overlap adjacent pieces 50 mm (2 in.) and roll all seams with a hand roller.

5.	Trim bottom edge 13 mm (1⁄2 in.) back from exposed face of the wall. Flashing shall not be permanently exposed to sunlight.

6. 	At heads, sills and all flashing terminations turn up ends a minimum of 50 mm (2 in.) and make careful folds to form an end dam, with the seams sealed.

7. 	Do not expose flashing membrane to sunlight for more than one hundred and twenty days prior to enclosure.

C. 	Accessories:

1. 	When required by dirty or dusty site conditions or by surfaces having irregular or rough texture, apply by air spray, brush or roller or apply primer by brush or roller at the rate recommended by manufacturer, prior to flashing installation. Allow the primer to dry completely before flashing application.