SECTION 07 6526.13

SELF-ADHERING STAINLESS STEEL SHEET MEMBRANE

PART 1  GENERAL

1.01	SECTION INCLUDES

A.	Flexible metal sheet membrane, including:

1.	Flexible stainless steel metal sheet, self-adhering type.

2.	Other specified system accessories.

1.02	REFERENCE STANDARDS

A.	AAMA 711 - Voluntary Specification for Self-Adhering Flashing Used for Installation of Exterior Wall Fenestration Products.

B.	ASTM A240/A240M - Standard Specification for Chromium and Chromium-Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels and for General Applications.

C.	ASTM D3273 - Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.

D.	ASTM D903 - Standard Test Method for Peel or Stripping Strength of Adhesive Bonds.

E.	ASTM E154/E154M - Standard Test Methods for Water Vapor Retarders Used in Contact with Earth Under Concrete Slabs, on Walls, or as Ground Cover.

F.	ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

G.	ASTM E96/E96M - Standard Test Methods for Water Vapor Transmission of Materials.

H.	ASTM E2178 - Standard Test Method for Air Permeance of Building Materials.

1.03	ADMINISTRATIVE REQUIREMENTS

A.	Coordination:

1.	Coordinate the installation of flexible metal sheet membrane with adjacent flashings, waterproofing systems, and other weather barriers for compatibility and continuity of those systems.

2.	Coordinate installation of flexible metal sheet membrane at openings with Sections that specify window, door, and other opening installations.

B.	Preinstallation Meeting:  Conduct a preinstallation meeting one week prior to the start of the work of this Section; require attendance by all affected installers.

1.	Convene under general provisions of Section 01 7000.

2.	Discuss installation procedures, requirements for items that penetrate the system, and other pertinent issues.

1.04	SUBMITTALS

A.	Product Data:  Provide data on material characteristics, performance criteria, and limitations.

B.	Shop Drawings:  Provide drawings of special joint conditions, including special conditions where incompatible materials are in close proximity to or in contact with specified flexible metal sheet flashings.

C.	Manufacturer's Installation Instructions:  Indicate installation methods, and storage and handling criteria.

1.05	QUALITY ASSURANCE

A.	Installer Qualifications:  Company specializing in performing the work of this Section with minimum three years documented experience, and approved by manufacturer.

B.	System Compatibility:  Assume responsibility for confirming that flexible metal sheet membrane is compatible with substrate surfaces with which they will be in contact, including but not limited to wall and sheathing surfaces, opening materials, waterproofing systems, other flashings and weather barrier materials, and sealants.

1.	Assure that system components are compatible as specified prior to preparing and making specified submittals.

2.	Assume responsibility for removal of incompatible system components and installation of properly compatible components at no additional cost to Owner regardless of when incompatibility is discovered.

C.	Basis of Design:  Specifications are based on flexible metal sheet membrane products by specified basis of design manufacturer.  Flexible metal sheet membrane products manufactured by other acceptable manufacturers are permitted, subject to compliance with specified requirements; and provided that deviations in design and performance are minor, and do not detract substantially from the indicated design intent.

1.06	MOCK-UPS

A.	Mock-up:  Construct mock-up of representative installation condition(s) as directed by Architect, approximately 4 feet long, indicating installation conditions including end dam condition at sill flashing application, if applicable.

1.	Locate where directed.

2.	Mock-up may remain as part of work.

PART 2  PRODUCTS

2.01	FLEXIBLE METAL SHEET FLASHINGS

=================================================================================

<<<<  PRODUCT IS "YORK 304 SA" FOR TYPE 304 STAINLESS STEEL; "YORK 316 SA" FOR TYPE 316 STAINLESS STEEL.

<<<<  RETAIN ONLY SALIENT CHARACTERISTIC PARAGRAPHS THAT ARE RELEVANT TO APPLICATION.

=================================================================================

A.	Flexible Metal Sheet Membrane:  Self-adhering, composite metal membrane composed of un-coated (bare) stainless steel sheet, butyl adhesive, and siliconized release liner; inherently compatible with all known air barrier sheets, membranes, and coatings, and requiring no substrate surface primers prior to installation.

1.	Stainless Steel Sheet:  ASTM A240/A240M, Type 304 alloy, 2 mil, 0.002 inch thick; smooth No. 4 (matte) finish.

a.	Sheet Width:  Minimum 4 inch, Maximum 36 inch.

2.	Adhesive: Block copolymer

3.	Air Permeability:  Pass; tested according to ASTM E2178.

4.	Vapor Retarder Classification:  Class 1, less than 0.1 perm; tested in accordance with ASTM E96/E96M.

5.	Puncture Resistance:  2,500 psi, minimum; tested in accordance with ASTM E154/E154M.

6.	Fastener Sealability:  Pass; tested in accordance with AAMA 711.

7.	Peel Adhesion to Substrates:  Minimum 3.5 lbf/in on application substrates; minimum 6.7 lbf/in for products applied to stainless steel air barrier membrane surfaces; tested in accordance with ASTM D903.

8.	Fire Resistance:  Pass, Class A; tested in accordance with ASTM E84.

9.	Mold Resistance:  Pass; tested in accordance with ASTM D3273.

10.	Basis of Design Product:

a.	York Manufacturing, Inc.; York 304 SA:  www.yorkflashings.com/.

11.	Other Acceptable Products:

a.	Momentive Performance Materials, Inc./GE Silicones; GE Elemax SS Flashing:  www.siliconeforbuilding.com/#sle.

b.	VaproShield, LLC; VaproThru-Wall Flashing SA:  www.vaproshield.com/#sle.

c.	Substitutions:  Permitted in accordance with Substitution Procedures specified in Division 01.

B.	Accessory Components:  As recommended by manufacturer for indicated applications.

PART 3  EXECUTION

3.01	EXAMINATION

A.	Verify that surfaces and conditions are ready for work of this Section.

B.	Where existing conditions are responsibility of another installer, notify Architect of unsatisfactory conditions.

C.	Do not proceed with this work until unsatisfactory conditions have been corrected.

3.02	PREPARATION

A.	Remove projections, protruding fasteners, and loose or foreign matter that might interfere with proper installation.

3.03	INSTALLATION

A.	General:  Install self-adhering flexible metal sheet membrane materials in accordance with manufacturer's published installation instructions for each indicated application.

1.	Installation instructions are available at https://www.yorkflashings.com/york-304-sa-self-adhering-stainless-steel-installation-instruction.

==========================================================================

<<<<  SELECT FROM BELOW AND EDIT TO SUIT PROJECT CONDITIONS.

==========================================================================

B.	Self-Adhering Flexible Metal Sheet Flashing:

1.	Applications:  Transition conditions between incompatible air barrier systems, including but not limited to transitions between:

a.	Air barrier sheets and fluid-applied air barrier membranes.

b.	Incompatible air barrier sheets.

c.	Incompatible air barrier membranes, coatings, and sealers.

d.	Other transition conditions as indicated on Drawings.

2.	Comply with manufacturer's protocols and special application instructions, particularly for cold-weather applications.

3.	Lap sheets shingle fashion to shed water, and seal laps airtight.

3.04	FIELD QUALITY CONTROL

A.	See Section 01 4000 - Quality Requirements for additional requirements.

B.	Do not cover installed membrane until required inspections have been completed.

C.	Obtain approval of installation procedures from membrane manufacturer based on a mock-up installed in place, prior to proceeding with remainder of installation.

D.	Take digital photographs of each portion of installation prior to covering up installed flashings.

3.05	PROTECTION

A.	Protect installed membranes from damage and integrity of sheet metal layer until covered by subsequent construction.

END OF SECTION